Understanding and Mitigating Iodide-Induced Surface Reactions on NiO for Stable Perovskite Solar Cells”

Nickel oxide (NiO) is a widely used hole-transport layer in inverted perovskite solar cells, but its chemical reactivity with iodide species can destabilize the NiO/perovskite interface. This work investigates how NiO thin films respond to hydrogen iodide (HI) and methylammonium iodide (MAI) under controlled thermal conditions (80–150 °C), both with and without protective surface layers. HI exposure produced a delayed surface reaction characterized by residue formation, thin-film interference patterns, and decreased contact angle, while HCl caused no observable changes, confirming iodide-specific reactivity. UV–vis and XRF analysis indicate that the reaction layer is extremely thin, consistent with surface-localized iodide interactions rather than bulk NiO etching. Protective interlayers significantly reduced or eliminated these effects, demonstrating their ability to suppress NiO surface reduction and iodide-induced modification. Finally, optimized NiO interfaces were integrated into full perovskite solar cells to evaluate device-level impact. These findings clarify the mechanism of NiO–iodide interaction and highlight practical strategies for stabilizing NiO-based perovskite architectures.